## Slide 1
Designing a Beam Under Messy Physics
ME 323 Module 1 — Lecture 1
Pick a 3D-printed I-beam that carries the most load per gram. The equations give you a start, not the answer.

## Slide 2
The challenge
  • Fixed: total height 18 mm, flange width 10 mm, test span 150 mm, printed length 172 mm, PLA.
  • You choose: web thickness b and web height H_web (which sets flange thickness).
  • Goal: maximize strength-to-weight.
  • Constraint you can't dodge: each print-and-test is slow and expensive, so you get very few.

## Slide 3
The challenge

## Slide 4
Why this is hard
Three things stand between you and a clean optimization:
  • Printed beams can fracture along the layer lines: the flange peels off the web at a printed interface whose strength appears in no handbook.
  • Lateral-torsional buckling depends on the fixture, not just the beam.
  • The failure modes overlap. Real beams fail in mixed, progressive ways.
We will price the layer-line mode with one calibrated number — but that number drifts with print session and support condition, and the other two problems remain. The equations narrow the problem without solving it.

## Slide 5
Three modeled capacity branches
  • Bending: the beam yields in flexure.
  • Flange-web separation: the shear flow at the printed junction exceeds the layer-line bond strength.
  • Lateral-torsional buckling (LTB): the beam tips over sideways.
The class capacity is the plain minimum of the three. The dominant-mode label is a model proxy, not proof of the observed fracture.

## Slide 6
Bending

## Slide 7
Why I-beams work
Bending strength is carried by I_x, and I_x counts each bit of area by the square of its distance from the neutral axis.
Material at the edges earns its mass; material near the center barely helps.
So put the mass in flanges far out, top and bottom. The web holds them apart (sets the lever arm) and carries the shear.
Maximize I_x per gram: that is the strength-to-weight game this module plays.

## Slide 8
Same mass, more stiffness
Three sections of equal area. Relocating the same material to the flanges multiplies I_x.
Even against a solid bar of the same height, the I-beam wins: its mass sits at the extreme fibers.

## Slide 9
The catch
The I-beam logic says: thinner web, taller section, mass pushed outward.
Push too far and you wake the other two modes:
  • a flange-web junction too thin to carry the shear flow — the printed layer-line bond lets go,
  • a section too tall and narrow, which tips over (LTB) before it ever yields.
The efficient shape and the failure modes pull against each other; resolving that tension is the design problem.

## Slide 10
Flange-web separation: shear flow at the printed junction
Every observed shear-type failure is a flange peeling off the web. The stress on that plane is the classic built-up-beam shear flow (V = P/2).

## Slide 11
What the separation check assumes
The stress measure is textbook mechanics — the same glue-line check used for any built-up member.
The strength side is not: tau_i is the bond strength along the printed layer lines, weaker than the bulk plastic, listed in no handbook.
Pre-lab 1 starts it at the bulk guess sigma_y/sqrt(3) = 43.9 MPa and calibrates it from the data — it lands near 18 MPa, and it drifts with print session and support condition.
The check predicts a capacity trend on one candidate plane. It is a dominant-mode proxy, not a fracture diagnosis.

## Slide 12
Fracture vs yield, on the test machine
Same fixture, same material. Thin webs shed the load in one drop; thicker webs plateau.
No equation on the previous slides distinguishes these two endings.

## Slide 13
Lateral-torsional buckling: the idea
A tall, thin-flanged beam does not yield in place. It rolls sideways and twists at a load below its bending strength — a stability failure, not a strength one.
The elastic critical moment, in the Eurocode C1/C2 closed form (Timoshenko elastic-stability theory).
The next four slides open up every symbol, because LTB decides your optimum and rests on the most assumptions.
You will not re-derive any of it: P_LTB arrives pre-coded in Pre-lab 1. The goal is to read that code knowing what each symbol assumes.

## Slide 14
The critical moment, term by term
Under the root, three effects trade against each other:
C_w / I_y — warping rigidity: the flanges resisting counter-bending.
L_b^2 GJ / (pi^2 E I_y) — St. Venant torsion: the open section's twisting stiffness.
(C_2 z_g)^2 — load height: loading the top flange is destabilizing, so it subtracts.
C_1 = 1.35 (central point load), C_2 = 0.55 (load-height factor).

## Slide 15
From critical moment to a load
The beam cannot exceed its yield moment, so LTB is capped at yield:
take the smaller of the elastic buckling moment and the yield moment,
convert moment to load with M_max = PL/4, so P = 4M / L,
with L_b = kL and z_g = c = TH/2 (load at the top surface).
The min is a crude nod to inelastic buckling.

## Slide 16
What feeds it: the section constants
  • I_y: weak-axis stiffness — small for narrow flanges, which is why tall thin beams tip.
  • J: St. Venant torsion, summed over web and flanges as thin rectangles.
  • C_w: warping constant, the flanges' resistance to counter-bending.
All three come from section_props in Pre-lab 1.

## Slide 17
The assumptions underneath
The formula is exact for an idealized beam, and ours differs from it in four ways.
  • Thin-walled open section: J and C_w use thin-rectangle theory. Webs up to 7 mm against a 10 mm flange stretch 'thin'; J drifts.
  • Timoshenko elastic stability: M_cr assumes linear-elastic, perfectly straight, no residual stress. A print has all three imperfections.
  • Warping torsion: the C_w term assumes ends free to warp. The real fixture restrains them — which is what k absorbs.
  • Elastic, isotropic material: E = 2.5 GPa, G = E/2.6 (nu = 0.3). Printed PLA is layered and anisotropic.
Each gap widens the error bar you should carry on the LTB capacity.

## Slide 18
The one number that rules LTB: k
k is the effective-length factor: how far the beam twists and bends sideways between whatever restrains it.
Set by the fixture — how the ends grip, whether they warp, where load lands — not by the beam.
Textbook k = 1 is a simply-supported fork end free to warp; stiffer restraint drops k below 1.
Handbook starting value k = 0.33. Calibration on the class subset gives k = 0.377, which sets the equation design.
Since M_cr ~ 1/k^2, a small change swings LTB hard — and the calibrated equation optimum sits on a bend-LTB knife edge (capacities within ~1%). k does not transfer between fixtures: confirm it on ours before betting on that optimum.

## Slide 19
LTB: what you must own, and what is background
You just saw Iy, J, Cw, warping, load height, and effective length. You are responsible for this much of it:
  • Yours: what LTB is (a tall thin web tipping sideways before the material yields), when it competes (thin b, large H_web), what k means physically, and why a calibrated k does not transfer between fixtures.
  • Yours: reading the capacity plot — which branch governs where, and how much margin the runner-up has.
  • Background: deriving Iy, J, Cw, or the Mcr formula. The code is supplied; you will never derive or re-implement it in this module.
The test of understanding: what happens to the LTB branch if the fixture braces the compression flange, and would you still trust the equation optimum?

## Slide 20
Which mode drives?
Tall thin webs tip (LTB). Short thin webs are separation-limited: junction shear flow beats the layer-line bond. The middle bends.

## Slide 21
Does the theory match the data?
Pre-lab 1 answers this with your beam dataset: compute each beam's predicted capacity and mode, then plot predictions against measurements.
Watch for two things:
  • Points below the line: beams that broke before the equations said they would.
  • Beams whose recorded failure looks nothing like the predicted mode.
[Placeholder: parity plot from the 44-beam dataset once strength_N lands.]

## Slide 22
One assumption, two different beams
Illustration: handbook starting values versus the class calibration (66.8 MPa, k = 0.377, tau_i = 16.8 MPa), which moves the equation optimum to (1.10, 13.25).

## Slide 23
Where this leaves us
The equations are useful but partial:
  • they cannot tell a yield plateau from a one-drop fracture,
  • their LTB term rests on fixture assumptions,
  • the modes blur,
  • and we have only a few expensive tests.
A data-driven model that carries its own uncertainty is built for this. Next lecture: Gaussian Processes and Bayesian optimization.

## Slide 24
The loop this module runs
Physics says what should happen and where failure lives. The data model says what the tests support and where we're still uncertain. Your judgment decides what to build. The test says what we got wrong.

## Slide 25
Before next time: Pre-lab 1
In ME323_Module1_Prelab1_FailureModes:
  • reduce four raw force-displacement traces to strength — including deciding what beam 9's "twisted off the test stand" peak really measures,
  • load the beam data, compute strength-to-weight,
  • code flexural yield and the junction shear-flow separation check (start tau_i at the bulk guess 43.9 MPa),
  • compare dominant-mode proxies with measured strengths and failure notes, then calibrate (sigma_y, k, tau_i),
  • optimize strength-to-weight.
The design you find there becomes one of the class's two ground-truth queries later — the pre-lab explains how those queries work. Bring questions.